## AISE SPERC fact sheet - Industrial use of Me-salts in Conversion Coating

| Section | Content |
| --- | --- |
| SPERC Title | Industrial use of Metal Salts in conversion coating |
| SPERC code |  |
|  | AISE SPERC 5.1a.v2 – Industrial use of Me-salts in Conversion Coating – Nickel AISE SPERC 5.1.b.v2 – Industrial use of Me-salts in Conversion Coating – Zinc, Chromium, Copper, Manganese |
| Scope |  |
|  | Covers the use of metal salts in a broad range of specific applications, e.g. surface treatment, metal treatment, surface finishing, corrosion inhibition etc. This includes the core process of treating the metal substrate as well as those processes required to support the core process such as storing, mixing, equipment cleaning, maintenance and associated laboratory activities. The treatment of the metal parts can occur by bathing or by spraying. The SPERCs are relevant for operations which discharge their wastewater to treatment by a municipal sewage treatment plant. Substance Domain: Metal salts |
| Related use descriptors |  |
|  | Main User Group: SU 3 |
|  | Sector of Use: |
|  | Environmental Release Class: ERC 5 |
|  | Process Categories: PROC2, PROC3, PROC4, PROC5, PROC7, PROC8a, PROC8b, PROC9 PROC10, PROC13, PROC15. |
|  | Product categories: PC 14 |
| Operational conditions |  | Operational conditions – Phrases |
|  | AISE 5.1a.v2 AISE 5.1.b.v2 | Indoor Use. Water-Based Process. Product applied in aqueous process solution with negligible volatilization. Spent fluid discharged to wastewater. |
|  |  | Operational conditions - Free text background |
|  | AISE 5.1a.v2 AISE 5.1.b.v2 | General good practice: e.g. trained staff, spill protection including waste reuse. Sites are operated to meet the local requirements for emissions of metals. Reduced emissions to waste water due to e.g.: Re-use of rinsing water The metal salts are dissolved in a water-borne application fluid, which is kept in a reservoir. It is pumped to dedicated machine(s) in order to be applied to the substrate or it is kept in a bath. With each piece of substrate a fraction of the application fluid is carried-over from the treatment bath. Via a sequence of rinsing steps this fraction of the application fluid is continuously emitted to the wastewater. |
| Obligatory onsite RMMs |  | RMM - Phrase | RMM-Efficiency (RESPERC) |
|  | AISE 5.1a.v2 | pH adjustment, and precipitation | 95 |
|  | AISE 5.1.b.v2 |  | 99 |
| Substance use rate |  | Phrase | Value |
|  | AISE 5.1a.v2 AISE 5.1.b.v2 | Indicative substance use rate in a typical operation (MSPERC in kg/d) | 50 |
|  | Justification |
|  | MSPERC-represents an indicative worst case value for the substance use rate per site. The amount of metal salt used for the daily replenishment constitutes the substance use rate. The rinsing of the metal parts results in a loss of process water. The volume of process water lost by rinsing is continuously each day and the concentration of the metal salts is adjusted accordingly. See MSPERC-derivation in Appendix. |
| Days emitting |  | Phrase | Value |
|  | AISE 5.1a.v2 AISE 5.1.b.v2 | Emission Days (days/year): | 220 |
| Release factors |  | Values (per pathway) |
|  |  | To air | To water | To soil | To waste |
|  | AISE 5.1a.v2 | 0 | 0.05 | 0 | 0.95 |
|  | AISE 5.1.b.v2 | 0 | 0.01 | 0 | 0.99 |
|  |  | Justification |
|  | Releases to Air: Metal salts in aqueous solutions are involatile and are intended to remain in the application solution. Volatilization of metal salts is therefore negligible. Spray applications are housed-in for the sake of worker protection. For the reasons above, the release factor to air is set to zero. Releases to water via wastewater: The spent process fluid consists of the rinsing, which contain the metal salts. As a first conservative approximation it assumed that the amount of metal salt is quantitatively lost from the process to the spent process water. Releases to soil: Releases to soil do not occur during normal operation of the process. Releases to waste: The treatment of the spent process fluids by pH-adjustment and subsequent filtration/sedimentation results in slurries or solid waste which is treated off-site. The content of the reservoir is disposed of once or twice per year and is treated off-site. |
| Optional risk management measures |  | Type of RMM | Efficiency |
|  | AISE 5.1a.v2 | pH adjustment and Sedimentation of solids by air flotation | 95 |
|  | AISE 5.1.b.v2 |  | 99 |
|  | AISE 5.1a.v2 | pH adjustment and Sedimentation of solids by filtration | 95 |
|  | AISE 5.1.b.v2 |  | 99 |
|  | The optional risk management measures listed here are technical alternatives to the RMMs listed under the obligatory on-site risk management measures. |
| Narrative description | Industrial Use of Metal Salts |
|  | This SPERC describes SPERC parameters relevant to the Industrial Use of Metal Salts in a water-based process for surface treatment, surface finishing, conversion coating etc. |
| Scaling | Scalable parameters | Parameter description | Values – SPERC /ES |
|  | MSite, SPERC (kg/d) | Amount which can be safely used based on the SPERC | MSafe (kg/d) – outcome of chemical safety assessment |
|  | RETotal, SPERC | Removal efficiency assumed in the SPERC | 0 |
|  | AISE 5.1a.v2 |  | 0.95 |
|  | AISE 5.1.b.v2 |  | 0.99 |
|  | QSPERC | Factor by which receiving surface water dilutes the sewage after treatment | 10 |
|  | GEffluent, SPERC (m3/d) | Volume of sewage treated per day (m3/d) | 2.000 |
|  |  | Scaling condition |
|  |  | risk driven by wastewater treatment plant microbes [MSite,SPERC x (1 – RETotal, SPERC )] / GEffluent, SPERC ( [MSite,Site x (1 – RETotal, Site)] / GEffluent, Site |
|  |  | risk driven by freshwater/freshwater sediments, marine water/marine water sediments [MSite,SPERC x (1 – RETotal, SPERC )] / (GEffluent, SPERC x qSPERC ) ( [MSite,Site x (1 – RETotal, Site)] / (GEffluent, Site x qSite) |
|  | Site-specific parameters | Parameter description | Values – Site |
|  | MSite, Site (kg/d) | Amount which is actually used on-site | To be determined by Downstream User |
|  | RETotal, Site | Removal efficiency realized through RMMs on site |  |
|  | qSite | Factor by which receiving surface water.dilutes the sewage after treatment |  |
|  | GEffluent, Site | Volume of sewage treated per day (m3/d). |  |

### Appendix: MSPERC-Derivation

*MSPERC is calculated according to: MSPERC  = Q Applicaton Fluid x CSP x FDilution . Wi th CSP = Concentration of substance in finished product, Q Applicaton Fluid  = the consumption of application fluid, FDilution  = the factor by which the metal salt-containing product is diluted to yield the application fluid.

The numbers in parentheses are the MSPERC-values, which are recommended as starting values for environmental exposure assessments, provided no better information is available.

Table 1: Derivation of the default substance use rate MSPERC for Industrial use of Metal Salts in conversion coating. The derivation is based on 2 sets of typical values of the operational conditions for the various applications covered by this SPERC.

| SPERC | Other Operational Conditions – Phrase | Operational Conditions – Values for selected parameters expressing the operational conditions for the SPERC ‘industrial use – formulation of granular cleaning and maintenance products. |
| --- | --- | --- |
|  |  | MSPERC in kg/d | QAF Consumption of application fluid (m3/d) | CSP Substance concentration in product (in % weight) | FDilution % of product in application fluid |
| AISE 5.1a.v2 AISE 5.1.b.v2 |  | 50 | 5 | 25 | 4 |
|  |  | 50 | 5 | 10 | 10 |

### Appendix - Determinant Lists

### SPERC 5.1a.v2	AISE - Industrial use of Me-salts in Conversion Coating – Nickel

| Determinant Label | Quali-/ Quanti-tative | Value | Description of Value | Standard Phrase | Efficiency -if applicable |
| --- | --- | --- | --- | --- | --- |
| Type of Process | Qual | Substance applied in aqueous process solution with negligible volatilization |  | Product applied in aqueous process solution with negligible volatilization. |  |
| Indoor/outdoor use | Qual | Indoor Use |  | Indoor |  |
| Chemical waste - discontinuous generation | Qual | Spent process fluid to be disposed of as chemical waste | Processing fluid can be kept in reservoir or treatment baths. Periodically, the reservoirs are emptied of the spent reservoir fluid and refilled with fresh reservoir fluid. The spent reservoir fluid is treated as chemical waste.Operators minimize the frequency of exchanging the reservoir fluid to reduce the cost of process chemicals, waste treatment and equipment downtime. | Spent process fluid to be disposed of as chemical waste |  |
| Chemical waste - continuous generation | Qual | Spent fluid discharged to wastewater. |  | Spent process fluid discharged to wastewater. |  |
| Process efficiency | Qual | Optimized water use due to e.g.: Re-use of rinsing water |  | Maximize waste water reuse |  |
| On site treatment of wastewater | Quan | pH-adjustment and subsequent filtration / sedimentation – Ni-salts |  | Chemical precipitation or sedimentation or filtration or electrolysis or reverse osmosis or ion exchange | water: 95% |

### SPERC 5.1b.v2	AISE - Industrial use of Me-salts in Conversion Coating –Zinc, Chromium, Copper, Manganese

| Determinant Label | Quali-/ Quanti-tative | Value | Description of Value | Standard Phrase | Efficiency -if applicable |
| --- | --- | --- | --- | --- | --- |
| Type of Process | Qual | Substance applied in aqueous process solution with negligible volatilization |  | Product applied in aqueous process solution with negligible volatilization. |  |
| Indoor/outdoor use | Qual | Indoor Use |  | Indoor |  |
| Chemical waste - discontinuous generation | Qual | Spent process fluid to be disposed of as chemical waste | Processing fluid can be kept in reservoir or treatment baths. Periodically, the reservoirs are emptied of the spent reservoir fluid and refilled with fresh reservoir fluid. The spent reservoir fluid is treated as chemical waste. Operators minimize the frequency of exchanging the reservoir fluid to reduce the cost of process chemicals, waste treatment and equipment downtime. | Spent process fluid to be disposed of as chemical waste |  |
| Chemical waste - continuous generation | Qual | Spent fluid discharged to wastewater. |  | Spent process fluid discharged to wastewater. |  |
| Process efficiency | Qual | Optimized water use due to e.g.: Re-use of rinsing water |  | Maximize waste water reuse |  |
| On site treatment of wastewater | Quan | pH-adjustment and subsequent filtration / sedimentation Metal salts other than Nickel |  | Chemical precipitation or sedimentation or filtration or electrolysis or reverse osmosis or ion exchange | water: 99% |